Supporting Information

Title Highly efficient slow-light Mach-Zehnder modulator achieving 0.21 V∙cm efficiency with bandwidth surpassing 110 GHz

Jian Shen,1,5 Yong Zhang,1,5,* Lei Zhang,1,5  Jingchi Li,1 Chenglong Feng,1 Yongheng Jiang,2 Hongwei Wang,1 Xingfeng Li,1 Yu He,1 Xingchen Ji,1 Guofeng Yin,3 Yonghui Tian,2 Xi Xiao,4 and Yikai Su1,*

*Corresponding Author: E-mail: yongzhang@sjtu.edu.cn, yikaisu@sjtu.edu.cn

1State Key Lab of Advanced Optical Communication Systems and Networks, Department of Electronic Engineering, Shanghai Jiao Tong University, Shanghai 200240, China

2Institute of Microelectronics and Key Laboratory for Magnetism and Magnetic Materials of MOE, School of Physical Science and Technology, Lanzhou University, Lanzhou 730000, Gansu, China

3Wuhan Enlarging Photonics Technology Co. LTD, Wuhan 430074, China

4National Information Optoelectronics Innovation Center, Wuhan 430074, Hubei, China

5These authors contributed equally.

1. Analysis for 1D slow-light waveguide

To investigate the slow-light effect in the waveguide, we start with a dielectric periodically stacked layers A and B, as depicted in Fig. 1(a). The refractive index ni and impedance zi with i = a, b can be expressed as1:

(1)

(2)

where the relative permittivity, relative permeability, refractive index, relative impedance, and width are defined as εa, εb, μa, μb, na, nb, za, zb, da, and db, respectively. According to transfer matrix method, the dispersion relation of the periodically stacked layers A and B can be achieved by[1]:

(3)

where the period of the unit cell is Λ = da+db, ki = niω/c (i = a, b), and q is the Bloch wave vector.

The sufficient condition and necessary condition for two band crossing is proved by the ratio of the optical path in A and B layer. The ratio can be expressed as:

(4)

where na and nb are refractive index of the layers A and B.

In the conclusion of the necessary condition, the frequency satisfied condition γ = mπ, m∊N+ (γ = (nada+nbdb)ω/c is the phase delay in a unit cell) must be within the band gap. If two bands cross at the condition of γ = mπ, the crossing points can be calculated as follows:

(5)

Therefore, the midgap positions can be labelled, which is related to the refractive index and width of the dielectric layers.

Figure S1. Index tailoring for slow-light lattice. (a) Schematic of the slow-light waveguide. Half a unit cell of the rectangular air holes for (b) B and (c) A layer. Relationship between the LN refractive index and effective index at (d) #1 and (e) #2 position. Insets are the mode profiles at position #1 and #2.

In our design, the periodic rectangular air holes are used to replace the stacked layers A and B, thus tailoring the effective refractive index of the integrated waveguides based on the SiN-loaded TFLN platform. The slow-light waveguide is depicted in Fig. S1(a) and the half a unit cell of the structure are illustrated in Fig. S1(b) and (c), where da = db = 0.5Λ.

The effective refractive index is calculated by using the effective-medium theory:

(6)

(7)

where neff1 and neff2 are the effective refractive indices at position #1 and #2. ρA and ρB are the duty cycle in the half a unit cell. The insets in Fig. S1(d) and (e) are the mode profiles at position #1 and #2. According to the finite element method, the relationship between the refractive index nLN and effective index neff1, neff2 can be fitted as follows:

(8)

(9)

where ε, θ, τ, φ is the linear fitting coefficients. For the SiN-loaded TFLN platform, the fitting values of ε, θ, τ, φ are determined as 0.62, 0.55, 0.78, 0.12, respectively. Consequently, a relationship between the refractive index of the layers A and B and the refractive index of the TFLN is established to evaluate the modulation efficiency of general Pockels modulators.

2. Tolerance of the slow-light structures

To verify the robustness of the slow-light waveguides to fabrication errors, additional simulations are performed. When the widths D1 and D2 of the 10 unit cells are varied within ±20 nm simultaneously, The transmission of the slow-light waveguide remains nearly unchanged, as shown in Fig. S2(a). Shifting the positions of the 10 unit cells downward or upward within a range of 20 nm results in a consistent bandgap position and transmission for the slow-light waveguide, as depicted in Fig. S2(b). This indicates a good tolerance of the slow-light waveguide in maintaining stability under fabrication variations.

Figure S2. Tolerance of the slow-light waveguide to fabrication errors. Transmission of the slow-light waveguide while (a) the widths D1 and D2 of the 10 unit cells are varied within ±20 nm simultaneously and (b) the positions of the 10 unit cells are shifted downward or upwards within 20 nm.

3. Comparison of AB rectangular holes lattice and Bragg gratings

In addition to improving the EO velocity and impedance matching (EO roll off), the proposed slow-light structure has some advantages in the EO modulation compared to conventional Bragg grating waveguides. We can consider the unit cell as “like-grating” structure, as illustrated in Fig. S3(a) and (b). These two structures can be considered as periodic modulations of the effective refractive index in the propagation direction of the optical mode, and each period contributes two reflections, as shown in Fig. S3(c).

Figure S3. Unit cell of the structures. (a) AB rectangular holes. (b) Bragg gratings. (c) Effective refractive index variations.

The periodic structures are used to couple forward-going and backward-going waves in the structures. According to coupled-mode theory, we can achieve the coupled-mode relationship:

(10)

(11)

where S and R are a sum of forward and backward propagating waves. κ is defined as the coupling coefficient of the structure. Δβ is the propagation constant deviation from the Bragg wavelength λB. For the periodic effective index variation, the coupling coefficient κ can be expressed as[2]:

(12)

where Λ is the period of the structure, neff is the effective refractive index without the structure, and effective refractive index variation Δn is neffa-neffb, which can be calculated by finite element simulation and effective-medium theory, as shown in Fig. S4(a).

Here, if the parameters D3=2ΔW in both structures for comparison, the effective refractive index variation increases when the parameters D3 or ΔW increases. According to Eq. (12), when the Bragg wavelength λB of both structures are simultaneously 1555 nm by the periodic adjustment, the coupling coefficients κ of the AB rectangular holes and the Bragg grating can be calculated. As illustrated in Fig. S4(b), the coupling coefficient κ of the AB rectangular holes is larger than that of the Bragg grating for the same ΔW perturbation.

Figure S4. Simulated coupling coefficients for comparison. (a) Calculated effective refractive index variations as a function of the perturbation width of the AB rectangular holes lattice and Bragg grating. (b) Calculated effective refractive index variation as a function of the coupling coefficient.

Compared to Bragg grating structure, a larger coupling coefficient κ has two advantages. First, the reflection can be improved. The reflection coefficient r for the structure with a length of L can be given as[3]:

(13)

(14)

In the case of Δβ=0, the peak reflectivity can be described as[3]:

(15)

As depicted in Fig. S5(a), the AB structure allows for larger reflections. It is expected that the length of the structure on the modulation arms can be further reduced.

Figure S5. Calculated results for comparisons. (a) Calculated amount of the reflection as a function of the length. (b) Calculated bandgap bandwidth as a function of the optical group index.

Second, a larger coupling coefficient κ can widen the bandgap, avoiding the closure. The bandwidth between the first nulls around the main reflection peak can be determined by:

(16)

for the long enough length (κ>>π/L), the bandwidth is primarily determined by κ, which can be rewritten as:

(17)

according to Eq. (17), the bandgap width of the AB rectangular holes lattice is larger than that of the Bragg grating, as illustrated in Fig. S5(b). The bandgap width decreases when the optical group index increases.

4. Perturbation theory for slow-light modulation efficiency

Modulation efficiency is crucial parameter for the integrated electro-optic modulators. The voltage-length product (Vπ∙L) is a commonly used figure of merit to characterize modulation efficiency, and it is primarily limited by the arm length, electrode gap, and electrode structure. In a Mach-Zehnder modulator (MZM), the induced phased shift on one arm can be mathematically described as follows[4]:

(18)

where ω is the angular frequency, k is the wavevector, and L is the arm length.

According to perturbation theory, the optical frequency shift of a photonic band at a fixed wavevector k caused by a small Δn can be estimated as[4]:

(19)

where σ represents the fraction of the mode energy in the region where Δn is applied, corresponding to the EO overlap factor. Considering the group velocity of light propagated in the waveguide:

(20)

which is much smaller than the speed of light c in vacuum. Therefore, according to Eq. (18) ~ (20), if the induced phase shift Δϕ = π/2, we can obtain:

(21)

when ω = 2πc/λ, where λ is the wavelength. Here, the phase shift is assumed as π/2, instead of π due to the push-pull configuration of the MZM. The change of LN refractive index Δn induced by the applied voltage Vπ can be achieved by:

(22)

where nLN is the LN refractive index, γ33 is the electro-optic coefficient of LN, g is the electrodes gap, and Ez is the in-plane component of the electrical field in the waveguide. The Vπ∙L can be calculated as:

(23)

According to Eq. (23), and (5) ~ (9), the Vπ∙L for the AB lattice slow-light waveguide can be written as:

(24)

when the period Λ and the duty cycle ρA, ρB of the air holes are designed as 420 nm, 0.38, and 0.71, respectively, the relationship between modulation efficiency Vπ∙L and wavelength group index ratio λ/ng is simulated and shown in Fig. S6. For the MZM, the wavelength group index ratio λ/ng can be adjusted to achieve a smaller Vπ∙L in the operation wavelength range.

Figure S6. Calculated modulation efficiency Vπ∙L as a function of λ/ng.

5. 1×2 multimode interference (MMI)

A MMI device serves as the fundamental unit for 3-dB optical power splitting and combining in an MZM. Based on the SiN-loaded TFLN platform, the multimode region is designed with a width of 10 μm and a length of 67 μm using the 3D-finite-difference-time-domain (3D-FDTD) method. Tapered waveguides with the widths of 1.6 μm and 3 μm are employed to connect the single-mode waveguide and the multimode region.

Fig. S7(a) displays scanning electron microscopy (SEM) images of the fabricated MMI device. The simulated electric field for the x-y region is depicted in Fig. S7(b). The input light is equally divided into two output ports, resulting in a balanced splitting ratio and low excess loss, as shown in Fig. S7(c). The simulated excess loss of the device is 0.19 dB, while the measured excess loss is 0.4 dB. The simulated power imbalance is 0.1 dB, while the measured power imbalance is 0.5 dB.

Figure S7. 1×2 MMI for 3-dB optical power splitter and combiner. (a) SEM of the MMI device. (b) Simulated mode profile of the MMI. (c) Measured transmission at port1 and port2 of the fabricated device.

6. Simulation of segmented slow-wave electrodes

To achieve a large EO bandwidth, factors such as low microwave loss, EO velocity and impedance matching are crucial considerations for MZM with traveling-wave electrodes. For EO velocity matching, it is important to ensure that the phase velocity of microwave signal matches the group velocity of the optical signal. This requires the microwave index should be equal with the optical group index.

In our design, slow-light effect in the waveguide with high group index is employed to achieve a high modulation efficiency, so that the increased microwave index controlled by the parameters of the T-shaped segmented slow-wave electrodes can match the optical group index to achieve a large bandwidth. The frequency response of the MZM with traveling-wave electrodes can be expressed as[5]:

(25)

where ω is the microwave angular frequency, L is the length of the electrode, Zin is the input impedance, F± are forward/backward propagating waves, and γm is the microwave propagation constant. These can be expressed as[6]:

(26)

(27)

where nm is the microwave index, ng is the optical group index, αm is the microwave loss rate, and c0 is the speed of light in vacuum.

According to Eq. (25) ~ (27), impedance matching (~ 50 Ω) can effectively reduce the microwave reflection, resulting in minimized standing waves and ripples in the EO frequency response. When nm ≈ ng, the microwave and optical signals can co-propagate at the same velocity, enabling the constructive modulation accumulation and frequency response enhancement.

To evaluate the electrical velocity of the T-shaped segmented slow-wave electrode, the controlled microwave index nm by the parameters of the T-shaped segmented slow-wave electrodes is simulated by finite element method. As illustrated in Fig. S8(a), the microwave index nm can be increased by increasing the length of T shape. Additionally, by reducing the electrodes gap and period, the microwave index nm can be increased, as shown in Fig. S8(b) and S8(c).

Considering modulation efficiency and index matching, the following electrode parameters are designed for the slow-light MZM: period p = 50 μm; side length h = t = 4 μm; electrode gap g = 5 μm; length of T shape r = 45 μm; width of T shape s = 2 μm. As depicted in Fig. S8(d), the simulated impedance is ~ 50 Ω, which is important to reduce the microwave reflections. The high modulation efficiency owing to the slow-light effect can effectively reduce the dependence on impedance matching. External sources with low voltages can be used to efficiently drive the electrodes.

We conduct a study on the impact of the substrates of the TFLN on microwave losses and electro-optic bandwidth. Assuming the electro-optic velocity and impedance matching, the microwave losses α of the T-shaped segmented slow-wave electrodes on the Si, air, and quartz substrate are simulated as 0.54, 0.22, and 0.31 dBcm-1GHz-1/2, respectively, corresponding to the EO S21 of <1 dB roll-off at 800 GHz, as illustrated in Fig. S8(e) and S8(f). When using an air substrate, the microwave loss is minimized, and the electro-optic bandwidth is maximized. The utilization of substrates with low permittivity or the undercut etching for the silicon substrates will lead to reduced microwave losses and increased electro-optic bandwidth.

Figure S8. Simulation of the T-shaped segmented slow-wave electrodes. Simulated microwave index with the variation of (a) length, (b) electrode gap, (c) period. (d) Simulated impedance under the different frequency. (e) Simulated Microwave loss on different substrates. (f) Estimated EO S21 curves on different substrates.

7. Discussion on the loss of the slow-light modulator

Due to the operating wavelength range near the bandgap, the on-chip losses of the device are wavelength-dependent. In the operational range of slow-light wavelengths spanning from 1544.9 nm to 1547.1 nm, the device demonstrates diverse levels of losses. These losses range from a maximum of 16.9 dB to a minimum insertion loss of 5.8 dB, as illustrated in Figure S9. The average insertion loss is calculated to be 9.3 dB. Achieving a low insertion loss within the slow-light region is anticipated through the implementation of cascaded topological cavities for modulation arms or a combination of strong bandgap widening and anticrossing effects[7].

Figure S9. Transmission at the operating wavelength slow-light wavelength region.

Here, we show an example of a slow-light structure with low loss and high group refractive index by cascading one-dimensional topological photonic crystal (1D-TPC) cavities. As shown in Fig. S10(a), assuming the number N of the single 1D-TPC cavity period is 60, the simulated transmission spectra are illustrated in Fig. S10(b) for the cascading 2, 3, 4, and 5 1D-TPC cavities. As the number of cascades cavity increases, the operation slow-light wavelength region increases and the insertion loss consistently remains below 1 dB. The optical group index can be calculated as[8]:

(28)

where λ is the centre wavelength, L is the length of the 1D TPCs, and Δλ is the peak spacing of the transmission.

This solution can achieve a slow-light operation region with a group index of approximately 6.8 within a bandwidth of 7.1 nm, while maintaining insertion loss of less than 1 dB. The careful selection and adjustment of the number N of periods play an important role in fine-tuning the group index. The group index can be further adjusted to meet specific requirements by tailoring the number N of periods.

Figure S10. Cascaded 1D-TPC cavities scheme. (a) Schematic diagram of cascaded 1D-TPC cavities. (b) Transmission of cascaded 1D-TPC cavities scheme.

8. Measured half-wave voltage at various wavelengths

Due to the strong dispersions around the Brillouin zone within the bandgap, the group index ng varies with the wavelength. Varying wavelengths can yield different Vπ in the 1-mm-length MZM. Fig. S11(a) exhibits the different Vπ at the wavelength of 1535 nm, 1546.1 nm, 1546.7 nm, 1546.92 nm. The Vπ of 2.1 V at the wavelength of 1547.1 nm is shown in Fig. 2(f) of the main content. The Vπ can be reduced from 21.7 V to 2.1 V as the wavelength is red-shifted from regular region to slow-light region. Consequently, the modulation efficiency Vπ∙L can be decreased from 2.17 V∙cm to 0.21 V∙cm. The corresponding extinction ratios are 22 dB, 23.2 dB, 23.8 dB, 23 dB, and 27.5 dB at the wavelength of 1535 nm, 1546.1 nm, 1546.7 nm, 1546.92 nm, and 1547.1 nm, respectively, as shown in Fig. S11(b).

Figure S11. Measured half-wave voltage Vπ for the 1-mm-length modulation arm. (a) Normalized optical transmission as a function of the applied voltage, showing Vπ of 21.7 V at the wavelength of 1535 nm, 9.8 V at the wavelength of 1546.1 nm, 7 V at the wavelength of 1546.7 nm, and 4 V at the wavelength of 1546.92 nm, respectively. (b) Optical transmission with the measured extinction ratio.

9. Measured S21 responses at various wavelengths

In the main text, we have plotted the S21 curves at various wavelengths (1546.1 nm, 1546.7 nm, 1546.92 nm, and 1547.1 nm), which correspond to modulation efficiencies of 0.98 V∙cm, 0.7 V∙cm, 0.4 V∙cm, and 0.21 V∙cm, respectively. Here, we give more experimentally measured S21 data at 0.3 nm intervals in the operation slow-light wavelength region from 1544.9 nm to 1547.1 nm, as illustrated in Fig. S12. It indicates that the modulation bandwidths are all exceeding 110 GHz in the slow-light region.

Figure S12. Measured EO S21 curves in the slow-light region.

10. Experimental setup for high bandwidth of >110 GHz

The experimental setup for the higher bandwidth test is shown in Fig. S13. In the case, the microwave signals with a frequency of >110 GHz are generated by beating two optical signals. Two tunable laser sources (TLS2 and TLS3) with different frequencies of f2 and f3 are used as two optical signals, which are combined by a 12 polarization-maintaining coupler. The combined signal is fed into a uni-travelling carrier photodiode (UTC-PD). Then, the microwave signal with the frequency |f2-f3| can be generated. Using the waveguide probe (WR5:140-220 GHz; WR6: 110-170 GHz), the microwave can be applied to the slow-light modulator. Finally, the intensity of the modulated sideband signals with different frequencies |f2-f3| can be analyzed by the optical spectrum analyzer (OSA), where the modulation bandwidth can be characterized.

Figure S13. Experimental setup for higher bandwidth test (140-220 GHz/110 GHz-170 GHz). TLS: tunable laser source; PMC: polarization-maintaining coupler; UTC-PD: uni-travelling carrier photodiode; EDFA: erbium-doped fiber amplifier; PC: polarization controller; OSA: optical spectrum analyzer.

11. Modulation energy consumption

For direct amplitude modulation, the energy per bit We dissipated in the modulator can be calculated as[9]:

(29)

where Vrms is the root-mean-square driving voltage, R is impedance, and r is the data rate. For 240 Gbps PAM4 signal modulation with a root-mean-square voltage Vrms of 730 mV, as shown in Fig. 4(g), the energy per bit We can be calculated as 44 fJ/bit.

12. Measured extinction ratios

We measure the extinction ratios of the device in the slow-light range from 1544.9 nm to 1547.1 nm. As shown in Fig. S14(a), there is a noticeable fluctuation in the extinction ratio. The minimum extinction ratio measured in the experiment at 1546 nm is 12.7 dB (Fig. S14(b)). The fluctuation in the extinction ratio is attributed to strong dispersion near the band edge of the topological photonic crystal, leading to non-ideal interference. Due to the variation in the extinction ratio, there is jitter in the bit error rate (BER) at different wavelengths in the slow light region.

Figure S14. Measured BERs and extinction ratios. (a) Measured BERs and extinction ratios in the slow-light region of the modulator. (b) Measured optical transmission as a function of the applied voltage at 1546 nm.

References

[1]. M. Xiao, Z. Q. Zhang, C. T. Chan, Physical Review X 2014, 4, 021017.

[2]. X. Wang, Ph.D. dissertation in The University Of British Columbia 2013.

[3]. X. Wang, W. Shi, H. Yun, S. Grist, N. A. F. Jaeger, and L. Chrostowski, Optics Express 2012, 20, 15547-15558.

[4]. M. Soljačić, S. G. Johnson, S. Fan, M. Ibanescu, E. Ippen, and J. D. Joannopoulos, Journal of the Optical Society of America B 2002, 19, 2052-2059.

[5]. M. He, M. Xu, Y. Ren, J. Jian, Z. Ruan, Y. Xu, S. Gao, S. Sun, X. Wen, L. Zhou, L. Liu, C. Guo, H. Chen, S. Yu, L. Liu, X. Cai, Nature Photonics 2019, 13, 359-364.

[6]. D. Zhu, L. Shao, M. Yu, R. Cheng, B. Desiatov, C. J. Xin, Y. Hu, J. Holzgrafe, S. Ghosh, A. Shams-Ansari, E. Puma, N. Sinclair, C. Reimer, M. Zhang, M. Lončar, Advances in Optics and Photonics 2021, 13.

[7]. A. Brimont, J. V. Galán, J. M. Escalante, J. Martí, and P. Sanchis, Optics Letters 2010, 35, 2708-2710.

[8]. T. Baba, Nature Photonics 2008, 2, 465-473.

[9]. C. Wang, M. Zhang, X. Chen, M. Bertrand, A. Shams-Ansari, S. Chandrasekhar, P. Winzer, M. Loncar, Nature 2018, 562, 101-104.